## Slide 1: Disorder in Graphene: Weak Localization

## Slide 2
Introduction
How to prepare Graphene: CVD
Experiment: Visualizing Weak Localization

## Slide 3: Background Knowledge and Introduction

## Slide 4: What is Graphene ?
Graphene is a two-dimensional material in which carbon atoms are arranged in a planar hexagonal lattice.
Graphene is an atomic scale material, so quantum mechanical effects are expected to be prominent. One such effect is “weak localization”.

## Slide 5: Weak Localization: Wave-particle duality
"Weak localization scattering" by A13ean - Own work. Licensed under CC BY-SA 3.0 via Wikimedia Commons - http://commons.wikimedia.org/wiki/File:Weak_localization_scattering.svg#/media/File:Weak_localization_scattering.svg
In Graphene, the wave property of electrons is noticeable in current-voltage characteristics.
When magnetic field is absent, due to constructive interference we expect increased possibility of electron at same point, which means lower current and higher resistance.
In presence of magnetic field, constructive interference is lost and resistance decreases.

## Slide 6: A closer look of weak localization
Hilke, Michael & Massicotte, Mathieu & Whiteway, Eric & Yu, Victor TheScientificWorldJournal, 2014, 737296--737296 (2014)

## Slide 7: How to prepare Graphene
The Development of Growing Graphene by CVD and Transferring method

## Slide 8: CVD: Chemical vapor deposition
In order to produce thin layer graphene, we need to expose metal film to hydrocarbon flow.
Yu, Q., Lian, J., Siriponglert, S., Li, H., Chen, Y. P., & Pei, S. S. (2008). Graphene segregated on Ni surfaces and transferred to insulators. Applied Physics Letters, 93(11), 113103.

## Slide 9: Further refinement of CVD
highly diluted hydrocarbon
Single-Crystalline Ni film
Thinner layer of metal material
Lee, Byeong-Joo, Han-Young Yu, and Goo-Hwan Jeong. "Controlled synthesis of monolayer graphene toward transparent flexible conductive film application."Nanoscale research letters 5.11 (2010): 1768-1773.

## Slide 10: Experiment Process

## Slide 11: Before Transfer: Multi layer Graphene on Copper and Nickle
From Graphene supermarket

## Slide 12: Transferring Process: Transfer Graphene On Copper to the substrate
1.wash sample with acetone
2.cover the sample with PMMA
3.heat the sample on metal
4.Desolve metal by acid
5.Transfer remaining PMMA to substrate
6.Heat
7.Remove PMMA by acetone

## Slide 17: Results Representation

## Slide 18: Raman Spectroscopy: Characteristic of Graphene
Childres, Isaac, et al. "Raman spectroscopy of graphene and related materials." Developments in photon and materials research (2013).

## Slide 19: Raman Spectroscopy: Defects of Graphene
Childres, Isaac, et al. "Raman spectroscopy of graphene and related materials." Developments in photon and materials research (2013).

## Slide 20: Raman Spectrum of Multilayer Graphene on cupper
Chart: Raman Spectrum of Graphene on Copper
Chart: Raman Spectrum of Graphene on Si

## Slide 21: CIP and CPP
CIP: Current in Plane geometry
CPP: Current Perpendicular to plane configuration
"Spin-valve CIP CPP" by Alex-engraver - Own work. Licensed under CC BY-SA 3.0 via Wikimedia Commons-http://commons.wikimedia.org/wiki/File:Spin-valve_CIP_CPP.svg#/media/File:Spin-valve_CIP_CPP.svg

## Slide 22: CIP Measurement
Chart: Resistance in varying temperature and magnetic field

## Slide 23: CPP Measurement
Chart: Resistance in varying temperature and magnetic field

## Slide 24: Test of circuit
Chart: Resistance at B=0T
| 2 | 1.9322029999999999 | 1.8644069999999999 | 1.79661 | 1.7288140000000001 | 1.661017 | 1.5932200000000001 | 1.5254239999999999 | 1.457627 | 1.3898299999999999 | 1.3220339999999999 | 1.254237 | 1.1864410000000001 | 1.118644 | 1.0508470000000001 | 0.9830508 | 0.91525420000000002 | 0.84745760000000003 | 0.77966100000000005 | 0.71186439999999995 | 0.64406779999999997 | 0.57627119999999998 | 0.5084746 | 0.44067800000000001 | 0.37288139999999997 | 0.30508469999999999 | 0.2372881 | 0.16949149999999999 | 0.1016949 | 3.3898310000000001E-2 | -3.3898310000000001E-2 | -0.1016949 | -0.16949149999999999 | -0.2372881 | -0.30508469999999999 | -0.37288139999999997 | -0.44067800000000001 | -0.5084746 | -0.57627119999999998 | -0.64406779999999997 | -0.71186439999999995 | -0.77966100000000005 | -0.84745760000000003 | -0.91525420000000002 | -0.9830508 | -1.0508470000000001 | -1.118644 | -1.1864410000000001 | -1.254237 | -1.3220339999999999 | -1.3898299999999999 | -1.457627 | -1.5254239999999999 | -1.5932200000000001 | -1.661017 | -1.7288140000000001 | -1.79661 | -1.8644069999999999 | -1.9322029999999999 | -2
10K | 0.064717 | 0.06238 | 0.060093 | 0.057844 | 0.055597 | 0.053373 | 0.051135 | 0.048901 | 0.046674 | 0.044519 | 0.042202 | 0.04001 | 0.037787 | 0.035579 | 0.033388 | 0.031196 | 0.029 | 0.026824 | 0.024692 | 0.02246 | 0.020295 | 0.018127 | 0.015968 | 0.013818 | 0.011673 | 0.0095306 | 0.0073999 | 0.0052833 | 0.0031563 | 0.0010466 | -0.0010635 | -0.003178 | -0.005303 | -0.0074378 | -0.0095716 | -0.011718 | -0.013876 | -0.016039 | -0.018208 | -0.020385 | -0.022569 | -0.024751 | -0.026958 | -0.029135 | -0.031312 | -0.033501 | -0.035657 | -0.037772 | -0.039916 | -0.042035 | -0.04417 | -0.046279 | -0.048395 | -0.050532 | -0.052662 | -0.054796 | -0.056898 | -0.058999 | -0.061131 | -0.063171
30K | 0.068227 | 0.06563 | 0.063202 | 0.060815 | 0.058453 | 0.056111 | 0.053728 | 0.051394 | 0.048994 | 0.04681 | 0.044326 | 0.041972 | 0.039648 | 0.037382 | 0.035046 | 0.032677 | 0.030435 | 0.028146 | 0.025912 | 0.023564 | 0.021287 | 0.019016 | 0.016756 | 0.014484 | 0.012223 | 0.0099947 | 0.0077641 | 0.0055383 | 0.0033094 | 0.0011 | -0.0011196 | -0.0033362 | -0.005562 | -0.0077944 | -0.01005 | -0.012303 | -0.01455 | -0.016817 | -0.01912 | -0.021396 | -0.02365 | -0.025981 | -0.028294 | -0.030602 | -0.032884 | -0.035152 | -0.037415 | -0.039672 | -0.041899 | -0.044105 | -0.046363 | -0.048672 | -0.050847 | -0.053121 | -0.055414 | -0.057658 | -0.059828 | -0.062137 | -0.064367 | -0.066679
60K | 0.070427 | 0.067802 | 0.065344 | 0.06286 | 0.060431 | 0.057987 | 0.055558 | 0.053143 | 0.050758 | 0.048453 | 0.045918 | 0.043452 | 0.04103 | 0.038648 | 0.036304 | 0.033891 | 0.03152 | 0.029156 | 0.026856 | 0.024399 | 0.022048 | 0.019694 | 0.017358 | 0.015026 | 0.012707 | 0.010384 | 0.0080619 | 0.0057531 | 0.0034369 | 0.0011429 | -0.001163 | -0.0034639 | -0.005775 | -0.0080977 | -0.010426 | -0.012756 | -0.015086 | -0.017427 | -0.01978 | -0.02217 | -0.024522 | -0.026905 | -0.029293 | -0.031687 | -0.033976 | -0.036316 | -0.038629 | -0.040971 | -0.043281 | -0.045642 | -0.047961 | -0.050266 | -0.052586 | -0.054839 | -0.057177 | -0.059497 | -0.061817 | -0.064159 | -0.066534 | -0.068828
100K | 0.07717 | 0.07433 | 0.071657 | 0.06897 | 0.066294 | 0.063628 | 0.060965 | 0.058309 | 0.055663 | 0.053135 | 0.050381 | 0.047736 | 0.045103 | 0.042477 | 0.039855 | 0.037242 | 0.034631 | 0.032032 | 0.029497 | 0.02684 | 0.024251 | 0.021674 | 0.019101 | 0.016534 | 0.013976 | 0.01142 | 0.0088772 | 0.0063451 | 0.0037951 | 0.0012617 | -0.0012841 | -0.0038214 | -0.0063643 | -0.0089129 | -0.011468 | -0.014033 | -0.016598 | -0.019174 | -0.021756 | -0.024342 | -0.026936 | -0.029537 | -0.032141 | -0.034697 | -0.03725 | -0.03978 | -0.04231 | -0.044825 | -0.047361 | -0.049887 | -0.052414 | -0.054932 | -0.057459 | -0.059961 | -0.062507 | -0.065006 | -0.067514 | -0.070033 | -0.072567 | -0.075077
150K | 0.07829 | 0.075428 | 0.072719 | 0.070017 | 0.067326 | 0.064629 | 0.061942 | 0.059254 | 0.056573 | 0.054019 | 0.05122 | 0.048548 | 0.045857 | 0.043216 | 0.040557 | 0.037906 | 0.035258 | 0.032614 | 0.030043 | 0.027343 | 0.024715 | 0.02209 | 0.019477 | 0.016866 | 0.014262 | 0.01166 | 0.0091011 | 0.0064818 | 0.0038778 | 0.0012905 | -0.0013123 | -0.0039051 | -0.0064995 | -0.0090997 | -0.011704 | -0.01431 | -0.016925 | -0.019545 | -0.022171 | -0.024802 | -0.027439 | -0.030079 | -0.032718 | -0.0353 | -0.037876 | -0.040447 | -0.043012 | -0.045563 | -0.048124 | -0.050678 | -0.05324 | -0.05577 | -0.058323 | -0.060876 | -0.063417 | -0.065974 | -0.068511 | -0.071016 | -0.073593 | -0.076098

## Slide 25: Assumption about absence of weak localization
1. Sample is too thick (sample behave like graphite)
2. Too few defects (too uniform)

## Slide 27: Creating more defects by hydrogen plasma
A new technic allows us to expand defects without etching graphene layers

## Slide 28: Comparison of graphene sample before and after hydrogen plasma bombardment
Chart: Raman of Graphene after bombardment
Chart: Raman of Graphene before bombardment

## Slide 29: CPP Measurement after defect creating
Chart: Resistance in varying temperature and magnetic field
| 10050.4 | 9575.6 | 9096.7999999999993 | 8611.2999999999993 | 8124 | 7632.5 | 7140.2 | 6646.4 | 6152.3 | 5651 | 5151.3999999999996 | 4649.1000000000004 | 4144.3999999999996 | 3638.7 | 3129.9 | 2622.3 | 2111.6999999999998 | 1602.82 | 1093.0899999999999 | 582.67999999999995 | 72.945999999999998 | -437.19 | -946.26 | -1454.2 | -1961.37 | -2467.3200000000002 | -2970.77 | -3474.7 | -3976 | -4479.8 | -4978.3 | -5477.5 | -5974.4 | -6468.1 | -6959.9 | -7451.7 | -7938 | -8421.7000000000007 | -8907.5 | -9387.7000000000007 | -9859.1 | -10330.200000000001 | -10793.9
15K | 23.7357 | 23.551 | 23.3502 | 23.1383 | 22.9302 | 22.7137 | 22.499 | 22.8809 | 22.6807 | 22.4661 | 22.25 | 21.995 | 21.7525 | 21.4641 | 20.6151 | 20.3785 | 20.1255 | 19.6313 | 19.4111 | 19.2329 | 19.0759 | 19.0104 | 19.0897 | 19.2146 | 20.0048 | 20.215 | 20.4526 | 20.6465 | 20.8541 | 21.0947 | 21.3339 | 21.5565 | 21.7454 | 22.0095 | 22.3532 | 22.5781 | 22.7951 | 22.9942 | 23.2201 | 23.4144 | 23.6177 | 23.8228 | 24.0213
30K | 25.2357 | 25.051 | 24.8502 | 24.6383 | 24.4302 | 24.2137 | 23.999 | 23.7809 | 23.5807 | 23.3661 | 23.15 | 22.895 | 22.6525 | 22.3641 | 22.1151 | 21.8785 | 21.6255 | 21.1313 | 20.9111 | 20.7329 | 20.5759 | 20.5104 | 20.5897 | 20.7146 | 20.9048 | 21.115 | 21.3526 | 21.5465 | 21.7541 | 21.9947 | 22.2339 | 22.4565 | 22.6454 | 22.9095 | 23.2532 | 23.4781 | 23.6951 | 23.8942 | 24.1201 | 24.3144 | 24.5177 | 24.7228 | 24.9213
60K | 33.7156 | 33.3889 | 33.0469 | 32.7318 | 32.3815 | 32.0266 | 31.6755 | 31.319 | 30.9636 | 30.5897 | 30.2584 | 29.9047 | 29.5429 | 29.2086 | 28.8611 | 28.5398 | 28.2196 | 27.9574 | 27.6931 | 27.4436 | 27.2488 | 27.0871 | 27.0262 | 27.0656 | 27.2033 | 27.3797 | 27.6133 | 27.867 | 28.1752 | 28.4688 | 28.7947 | 29.1186 | 29.8457 | 29.8618 | 30.1521 | 30.7199 | 30.9526 | 31.3029 | 31.5979 | 32.0521 | 32.324 | 32.6487 | 32.9703

## Slide 30: Test of circuit
Chart: Resistance at B=0T
| 2 | 1.9322029999999999 | 1.8644069999999999 | 1.79661 | 1.7288140000000001 | 1.661017 | 1.5932200000000001 | 1.5254239999999999 | 1.457627 | 1.3898299999999999 | 1.3220339999999999 | 1.254237 | 1.1864410000000001 | 1.118644 | 1.0508470000000001 | 0.9830508 | 0.91525420000000002 | 0.84745760000000003 | 0.77966100000000005 | 0.71186439999999995 | 0.64406779999999997 | 0.57627119999999998 | 0.5084746 | 0.44067800000000001 | 0.37288139999999997 | 0.30508469999999999 | 0.2372881 | 0.16949149999999999 | 0.1016949 | 3.3898310000000001E-2 | -3.3898310000000001E-2 | -0.1016949 | -0.16949149999999999 | -0.2372881 | -0.30508469999999999 | -0.37288139999999997 | -0.44067800000000001 | -0.5084746 | -0.57627119999999998 | -0.64406779999999997 | -0.71186439999999995 | -0.77966100000000005 | -0.84745760000000003 | -0.91525420000000002 | -0.9830508 | -1.0508470000000001 | -1.118644 | -1.1864410000000001 | -1.254237 | -1.3220339999999999 | -1.3898299999999999 | -1.457627 | -1.5254239999999999 | -1.5932200000000001 | -1.661017 | -1.7288140000000001 | -1.79661 | -1.8644069999999999 | -1.9322029999999999 | -2
Reading 15K | 0.09545 | 0.092514 | 0.088384 | 0.085922 | 0.082872 | 0.079667 | 0.076008 | 0.072926 | 0.066864 | 0.066727 | 0.063313 | 0.05874 | 0.055242 | 0.053413 | 0.050219 | 0.046908 | 0.043511 | 0.039136 | 0.03632 | 0.033908 | 0.0306 | 0.027339 | 0.024121 | 0.020916 | 0.017479 | 0.014461 | 0.011228 | 0.0059974 | 0.0047881 | 0.0015949 | -0.0016189 | -0.0048283 | -0.0080187 | -0.0109 | -0.014496 | -0.017763 | -0.020644 | -0.023902 | -0.027408 | -0.030662 | -0.033868 | -0.037055 | -0.039165 | -0.042354 | -0.046598 | -0.049628 | -0.052584 | -0.055889 | -0.059025 | -0.061414 | -0.065272 | -0.068172 | -0.071023 | -0.07412 | -0.077376 | -0.080476 | -0.083547 | -0.086276 | -0.085178 | -0.092633
Reading 30K | 0.096302 | 0.092665 | 0.089575 | 0.086304 | 0.083019 | 0.079546 | 0.076432 | 0.072028 | 0.069853 | 0.066757 | 0.063323 | 0.060042 | 0.056775 | 0.053464 | 0.049478 | 0.046927 | 0.043586 | 0.040226 | 0.037241 | 0.033907 | 0.030656 | 0.027417 | 0.024156 | 0.019917 | 0.017709 | 0.014483 | 0.011259 | 0.0080535 | 0.0048175 | 0.0016024 | -0.0016217 | -0.0048362 | -0.0078586 | -0.011293 | -0.014531 | -0.017764 | -0.020999 | -0.024241 | -0.027446 | -0.030435 | -0.033972 | -0.036965 | -0.040125 | -0.043449 | -0.046604 | -0.049713 | -0.052844 | -0.055943 | -0.06216 | -0.065272 | -0.068272 | -0.07146 | -0.074558 | -0.077623 | -0.080174 | -0.083642 | -0.085176 | -0.089724 | -0.09274
Reading 60K | 0.074062 | 0.070753 | 0.06884 | 0.066379 | 0.063856 | 0.061352 | 0.058838 | 0.056277 | 0.053642 | 0.051251 | 0.048293 | 0.046176 | 0.043625 | 0.041146 | 0.038641 | 0.036137 | 0.033605 | 0.030953 | 0.028623 | 0.026042 | 0.02347 | 0.021091 | 0.018601 | 0.016103 | 0.013633 | 0.011136 | 0.0085786 | 0.0061913 | 0.0037087 | 0.0012335 | -0.0012526 | -0.0037317 | -0.0062062 | -0.008675 | -0.011163 | -0.013559 | -0.016144 | -0.018648 | -0.021143 | -0.02365 | -0.026155 | -0.028644 | -0.031074 | -0.033578 | -0.035997 | -0.038389 | -0.040906 | -0.04332 | -0.045692 | -0.048127 | -0.050478 | -0.052726 | -0.055275 | -0.057723 | -0.060071 | -0.062467 | -0.064853 | -0.06712 | -0.069421 | -0.071807

## Slide 31: Thanking
Dr. Sandipan Pramanik and Dr. Srikrishna Chanakya Bodepudi have given a lot of help in this research.
Thanks to their consistent and effective guidance, this research can finally flow smoothly and successfully.

## Slide 32: Citation
R. V. Gorbachev, F. V. Tikhonenko, A. S. Mayorov, D. W. Horsell, and A. K. Savchenko, Phys. Rev. Lett. 98, 176805,2008,Apr 26
Datta, S. (1995). Electronic Transport in Mesoscopic Systems. Cambridge University Press.ISBN 0521599431.
A. H. Castro Neto, F. Guinea, N. M. R. Peres, K. S. Novoselov, and A. K. Geim, Rev. Mod. Phys. 81, 109 – Published 14 January 2009
Zhimin L, Hanchun W, Shishir K, Duesberg G S, Yangbo Z, Cross G L W, Shvets I V and Dapeng Y 2012 Adv. Mater. 24 1862

## Slide 33: Citation
Yu, Q.; Lian, J.; Siriponglert, S.; Li, H.; Chen, Y. P.; Pei, S.-S. Applied Physics Letters 2008,93, 113103–113103–3.
Reina, A.; Jia, X.; Ho, J.; Nezich, D.; Son, H.; Bulovic, V.; Dresselhaus, M. S.; Kong, J.Nano Lett. 2008, 9, 30–35.
Kim, K. S.; Zhao, Y.; Jang, H.; Lee, S. Y.; Kim, J. M.; Kim, K. S.; Ahn, J.-H.; Kim, P.;Choi, J.-Y.; Hong, B. H. Nature 2009, 457, 706–710.
Zhang, Y.; Gomez, L.; Ishikawa, F. N.; Madaria, A.; Ryu, K.; Wang, C.; Badmaev, A.;Zhou, C. J. Phys. Chem. Lett. 2010, 1, 3101–3107.

## Slide 34: Citation
Lee, Byeong-Joo, Han-Young Yu, and Goo-Hwan Jeong. "Controlled synthesis of monolayer graphene toward transparent flexible conductive film application." Nanoscale research letters 5.11 (2010): 1768-1773.
Hilke, Michael & Massicotte, Mathieu & Whiteway, Eric & Yu, Victor TheScientificWorldJournal, 2014, 737296--737296 (2014)
Childres, Isaac, et al. "Raman spectroscopy of graphene and related materials." Developments in photon and materials research (2013).

## Slide 35: A More Insight View
The weak localization effect manifests itself much stronger in low dimensional systems, since it is much more likely to find a self-crossing trajectory in low dimensions.[2]
Resistance is related to the probability of electron flowing from A to B.
As the result of trajectory interference, the probability that the electron goes back to the origin is enhanced, so the conductivity is reduced.[3]

## Slide 36: Grow "Graphene" on Ni
It has been discovered that graphene segregation could be adopted to deliver high quality graphene with large area.
The grown graphene could be easily transferred by using nitric acid.
  This transferring process is fairly easy ,economical and highly feasible.

## Slide 37: summary
Several layers of graphene had been synthesized on Ni substrates by a surface segregation process with controlled cooling and transferred to glass substrates.
TEM and Raman data showed that the graphene films can maintain their high quality even after being subject to the usage of HNO3 and various mechanical operations during the TEM sample preparation and substrate transfer.
Cooling rate found to be optimal and the quality of graphene films can be controlled by varying other growth conditions.
These results indicate that the surface segregation from metals in the ambient pressure with controlled cooling rates could offer a high quality and low cost synthesis approach for graphene as a practical electronic material.
Yu, Q.; Lian, J.; Siriponglert, S.; Li, H.; Chen, Y. P.; Pei, S.-S. Applied Physics Letters 2008,93, 113103–113103–3.

## Slide 38: Fewer Layers, More Substrate !
The CVD process has been refined by exposing Ni film to highly diluted hydrocarbon flow, which gave ultra thin graphene.
  This improvement has enabled researchers more ability to control the layer of graphene.
Transferring process was also improved by the wet-etching of the underlying Ni film. It made transferring graphene to random substrate available.
  By introducing a PMMA layer, the graphene can almost be transferred to any material. Comparing to the original process, this improvement enabled more substrates choice.

## Slide 39: summary
For the first time that continuous films with single-to few-layer graphene can be grown by ambient pressure CVD on polycrystalline Ni and transferred to a large variety of substrates.
The films exhibit a large fraction of single-and bilayer graphene regions with up to ~20 while remaining continuity and conductivity after numerous processing steps.
These films demonstrate a comparable structural quality to existing graphene materials but are fabricated without the need of bulk single crystal substrate or complex processing conditions.
The graphene film size is determined by the area of the Ni growth surface and is only limited by the CVD chamber size. This approach enables a viable route toward the scalable production of graphene structures for future applications.
Reina, A.; Jia, X.; Ho, J.; Nezich, D.; Son, H.; Bulovic, V.; Dresselhaus, M. S.; Kong, J.Nano Lett. 2008, 9, 30–35.

## Slide 40: Stretchable !
Some researchers used a nickel film of thickness of 300 nm to grow graphene. It produced a more uniformed monolayer/bilayer graphene. It allowed property of graphene film unchanged after mechanical stretch.
  By this method, graphene can be made more uniformed. Hence stretchability of graphene is enhanced.
A new transferring method was also developed. Instead of using acid, they found Iron (III) chloride more attempting. It improvement prevent graphene from being damaged by bubbles produced by acid.
  Instead of using acid, Using Iron (III) chloride gives graphene better protection during transferring process.

## Slide 41: summary
A simple method had been developed to grow and transfer high-quality stretchable graphene films on a large scale using CVD on nickel layers.
The patterned films can easily be transferred to stretchable substrates by simple contact method, and the number of graphene layers can be controlled by varying the thickness of the catalytic metals, the growth time and and/or the ultraviolet treatment time.
The graphene films enable numerous applications including use in large-scale flexible, stretchable, foldable transparent electronics.”
Kim, K. S.; Zhao, Y.; Jang, H.; Lee, S. Y.; Kim, J. M.; Kim, K. S.; Ahn, J.-H.; Kim, P.;Choi, J.-Y.; Hong, B. H. Nature 2009, 457, 706–710.

## Slide 42: Better Growth: Single-Crystalline Ni film
It was found that the formation for monolayer/bilayer graphene on the single crystal surface was much easier than that on polycrystalline Ni film. The secret was the nature of its smooth surface and absence of grain boundaries.
  Rather than using polycrystalline Ni film, single crystal Ni was adopted. It turned out that a smooth surface provides a better production of monolayer/bilayer graphene.

## Slide 43: summary
Preferential formation of monolayer/bilayer graphene on the single crystal surface is attributed to its atomically smooth surface and the absence of grain boundaries. In contrast, CVD graphene formed on polycrystalline Ni leads to higher percentage of multilayer graphene (3 layers), which is attributed to the presence of grain boundaries in Ni that can serve as nucleation sites for multilayer growth.
Zhang, Y.; Gomez, L.; Ishikawa, F. N.; Madaria, A.; Ryu, K.; Wang, C.; Badmaev, A.;Zhou, C. J. Phys. Chem. Lett. 2010, 1, 3101–3107.